Size(mm) : 915x1830 / 1200x2400 / 1220x2440 / 1250x2500 / 1500x2500 / 1500x3000

Thickness(mm) : 6.5 / 9 / 12 / 15 / 18 / 20 / 21 / 24 / 27 / 30 / 35

Length&width tolerance : +/-2mm

Number of layers : from 5 up to 21 depending on thickness

Core : Poplar , Hardwood , Birch , Pine , Combi

Water resistance : WBP(weather and water-proof)

| Inspected unit | SHANDONG XINGANG GROUP |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Product name | Film faced plywood |  | No.of layers | 11 |  |
| Product size | 2440×1220×18mm |  | Wood species | Eucalyptus |  |
| Testing date | 31th Mar,2021 |  | Standard | GB/T17656-2008 |  |
| Glue | Phenolic |  | Sample size | mm:600×1200×18 2pcs |  |
| Testing item |  | Unit | Normal value required | Tested value | Conclusion |
| Moisture content |  | % | 2023/6/14 | 7.5 | PASS |
| Density |  | Kg/m3 | 580-620 | 605 | PASS |
| Bonding quality | Mear shear strength(fV) | N/mm2 | ≥0.70 | Xmax:1.71 | PASS |
|  |  |  |  | Xmin:1.06 |  |
|  | Mean apparent percentage wood failure(W) | % | / | 70 | PASS |
| Bending strength | Longitudinal grain | N/mm2 | ≥35 | 70.12 | PASS |
|  | Cross grain | N/mm2 | ≥25 | 45.84 | PASS |
| Modulus of elasticity in bending | Longitudinal grain | N/mm2 | ≥5000 | 7250 | PASS |
|  | Cross grain | N/mm2 | ≥4000 | 5270 | PASS |
| remarks | Moisture content (specimen dimension:50mm×50mm×18mm; number: 6) |  |  |  |  |
|  | density(specimen dimension:50mm×50mm×18mm; number: 6) |  |  |  |  |
|  | Bonding quality(specimen dimension: 100mm×25mm×18mm; 10 test pieces per glueline) |  |  |  |  |
|  | Bending strength and Modulus of elasticity in bending (specimen dimension: 300mm×50mm×18mm; number: 6 with Longitudinal grain fibers and 6 with Cross grain fibers) |  |  |  |  |

| Sr No. | Property |  | Unit | Test Method | Value of Test | Result |
| --- | --- | --- | --- | --- | --- | --- |
| 1. | Moisture Content |  | % | EN 322 | 7.8 | Check out |
| 2. | Density |  | kg/m³ | EN 323 | 635 | Check out |
| 3. | Bonding Quality | Bonding Quality | Mpa | EN 314 | Max：1.68 Min ：0.81 | Check out |
|  |  | Damage Rate | % | —— | 85% |  |
| 4. | Bending Modulus of Elasticity | Longitudinal | Mpa | EN 310 | 6830 | Check out |
|  |  | Lateral |  |  | 6090 |  |
| 5. | Bending Strength N/mm | Longitudinal | Mpa |  | 59 | Check out |
|  |  | Lateral |  |  | 43.9 |  |
| 6. | Cycle Life | About 15-25 Repeated Using Times According to Projects by Formwork Application |  |  |  |  |

Tested Item Type： full hardwood film faced plywood 18mm.

Tested Item Type： full poplar film faced plywood 18mm.

| Sr No. | Property |  | Unit | Test Method | Value of Test | Result |
| --- | --- | --- | --- | --- | --- | --- |
| 1. | Moisture Content |  | % | EN 322 | 8.4 | Check out |
| 2. | Density |  | kg/m³ | EN 323 | 530 | Check out |
| 3. | Bonding Quality | Bonding Quality | Mpa | EN 314 | Max：1.40 Min ：0.70 | Check out |
|  |  | Damage Rate | % | —— | 74% |  |
| 4. | Bending Modulus of Elasticity | Longitudinal | Mpa | EN 310 | 5215 | Check out |
|  |  | Lateral |  |  | 4796 |  |
| 5. | Bending Strength N/mm | Longitudinal | Mpa |  | 52.74 | Check out |
|  |  | Lateral |  |  | 43.55 |  |
| 6. | Cycle Life | About 8-15 Repeated Using Times According to Projects by Formwork Application |  |  |  |  |

Tested Item Type： full birch film faced plywood 18mm.

| Sr No. | Property |  | Unit | Test Method | Value of Test | Result |
| --- | --- | --- | --- | --- | --- | --- |
| 1. | Moisture Content |  | % | EN 322 | 8.1 | Check out |
| 2. | Density |  | kg/m³ | EN 323 | 690 | Check out |
| 3. | Bonding Quality | Bonding Quality | Mpa | EN 314 | Max：1.85 Min ：0.99 | Check out |
|  |  | Damage Rate | % | —— | 94% |  |
| 4. | Bending Modulus of Elasticity | Longitudinal | Mpa | EN 310 | 9610 | Check out |
|  |  | Lateral |  |  | 7360 |  |
| 5. | Bending Strength N/mm | Longitudinal | Mpa |  | 79 | Check out |
|  |  | Lateral |  |  | 77.3 |  |
| 6. | Cycle Life | About 30-50 Repeated Using Times According to Projects by Formwork Application |  |  |  |  |

COLOR OF SURFACE/FILM:BLACK FILM,BROWN FILM,GREEN PLASTIC FILM

- Quality control:

We have 16 QC teams to inspection such as moisture control, glue inspection both before pro-duction and after production, material grade selection, pressing checking, and thickness che-cking. Our aim is to supply high quality product with reasonable price.

MORE PRODUCTS

- Finger-Jointed Film Faced Plywood

SIZE(MM):915X1830,1220X2440,1500X2500,1200X2400,1250X2500,1500X3000

THICKNESS(MM):9,12,15,18,20,21,24,27,30,35

- PP、PVC Plywood

SIZE(MM):915X1830,1220X2440,1500X2500,1200X2400,1250X2500,1500X3000

green pvc film / blue pvc film / yellow pvc film

- Anti-slip film faced plywood

COLOR OF SURFACE/FILM:BLACK FILM,BROWN FILM,GREEN PLASTIC FILM

GLUE:WBP MELAMINE,WBP PHENOLIC

CORE : BIRCH,POPLAR,HARDWOOD,PINE,COMBI

Plastic Plywood

PP,PVC Plywood

- To learn more about our products and services, contact us today!

- Add:Yitang Town,Lanshan District,Linyi City,Shandong Province,P.R.China

- Tel:0086-539-7053333               Fax:086-7052222

- Http://www.xingang-wood.com

- Email:xingang@cnxingang.cn